## Slide 1: Presentation on Sheet Metal Design

## Slide 2: Contents
Introduction
Metals used in Sheet Metal Working
Gauges
Sheet Metal Forming Processes
Comparison to other forming processes
Die Manufacturing
Progressive die with scrap strip and stamping
Die operations and types
Design calculations
For Blanking and Piercing
Draw Die Designing
Bending Design
Punching Design
Die Construction
Workshop Practice
Safety Guide for Sheet Metal Workers

## Slide 3: Introduction
Sheet metal is simply metal formed into thin and flat pieces. It is one of the fundamental forms used in metalworking, and can be cut and bent into a variety of different shapes.
The thickness of the sheet metal is called its gauge. The gauge of sheet metal ranges from 30 gauge to about 8 gauge
Sheet metal working involves manufacturing articles from sheet metal or thin sheets, which may be of black iron, galvanized iron, copper or stainless steel.

## Slide 4: Metals used in Sheet Metal Working
A large variety of metals in the form of sheets and plates used in sheet metal working include black iron, galvanized iron, copper, brass, tin, aluminum, lead and zinc.
The thickness of sheets vary inversely as their gauge number, higher the gauge number, smaller the thickness and vice-versa.
Important metals used in sheet metal working are described below. Black Iron Sheet or uncoated sheet is the cheapest material used for sheet metal work. Since these sheets carry no protection coatings on their surfaces, these are likely to corrode quickly.These are, therefore, used for marking those articles, which are later enamelled or painted before use.

## Slide 5: Gauge
The sheet metal gauge (sometimes spelled "gage") indicates the standard thickness of sheet metal for a specific material. As the gauge number increases, the material thickness decreases
Sheet metal thickness gauges for steel are based on a weight of 41.82 pounds per square foot per inch of thickness. This is known as the Manufacturers' Standard Gage for Sheet Steel.

## Slide 6: SHEET METAL FORMING PROCESSES
  Piercing
  Blanking
  Fine Blanking
  Punching
  Trimming
  Nibbling
  Notching
  Drawing
  Spinning
  Bending
  Embossing
  Coining

## Slide 7: BENDING
The bending operation is the act of bending blanks at a predetermined angle.
An example would be an "L" bracket which is a straight piece of metal bent at a 90° angle. The main difference between a forming operation and a bending operation is the bending operation creates a straight line bend (such as a corner in a box) as where a form operation may create a curved bend (such as the bottom of a drinks can).

## Slide 8: Bending and Press Brake Machines

## Slide 9: Comparison to other forming techniques
Other methods of forming round metal parts include hydroforming, stamping and forging or casting. Hydroforming and stamping generally have a higher fixed cost, but a lower variable cost than metal spinning. Forging or casting have a comparable fixed cost, but generally a higher variable cost. As machinery for commercial applications has improved, parts are being spun with thicker materials in excess of 1" thick steel. Conventional spinning also wastes a considerably smaller amount of material than other methods.

## Slide 10: Advantages
These are several benefits of spinning and shear forming. Several operations can be performed in one set-up.
Work pieces may have re-entrant profiles and the profile in relation to the center line virtually unrestricted.
Forming parameters and part geometry can be altered quickly, at less cost than traditional metal forming techniques.
Tooling and production costs are also comparatively low.
Spin forming is easily automated and an effective production method for prototypes as well as high production runs.

## Slide 11: Die (manufacturing)
A die is a specialized tool used in manufacturing industries to cut, shape and form a wide variety of products and components. Like molds and templates, dies are generally customized and uniquely matched to the product they are used to create. Products made with dies range from simple paper clips to complex pieces used in advanced technology.

## Slide 12: DESIGN CALCULATIONS

## Slide 13: For Blanking and Piercing
Clearences:
Clearences is one of the main factors controlling a shearing process. The clearence per side is given by
C=0.0032 . t . τ
Where
t= thickness and
τ= material shear stress, MPa
Angular Clearance:
Angular clearance or draft in a shearing operation depends on the material, thickness and shape of the stock used.
Its value ranges from 0.25 to 2 deg per side.

## Slide 14
Punching Force:
As the name indicates it is the force of the punch needed to cut the blank or pierce a sheet
F(p) = L . t . Τ
F(p)= punching force, N
τ =Shear strength MPa
For holes with diameter d<t
F(p)=D.t. s/3√D/t
Where, D= diameter of punch,mm
s = tensile strength in Mpa.

## Slide 15: Draw Die Design
Corner Radius on Punch:
Customery taken as 4t to 10 t and ideally taken as equal to punch radius.
Draw Radius:
Larger radius causes the metal to be released early by the blank holder and thus lead to edge wrinkling. Too small a radius causes the thinning and tearing of the side walls of the cups, generally,
Draw radius=4.t normal
=6 to 8 t when the blank holder is used.
Clearences:
An allowance in the range of 7 to 20% of the blank thickness is provided, depending on the cup material and cup dimensions.

## Slide 16
Blank Size:
The calculation could be based on volume, surface area or by layout. Some useful relations in calculating the blank diameter for cylindrical shell for relatively thin materials are given by:
D=√(d2+4dh) when d ≥20r
D=√(d2+4dh-0.5r) when 15r ≤d≤20r
D=√(d2+4dh-r) when 10r≤d≤15r
D=√((d-2r)2+4d(h-r)+2πr(d-0.7r)) when d<10r
Where
r = corner radius of the punch, mm
h = height of the shell, mm
d = outer diameter of the shell, mm
D = blank diameter, mm
An additional trim allowance could be provided of 3 mm per 25mm of cup diameters.

## Slide 17
Drawing Force:
Drawing force for cylindrical shapes can be given by the below empirical equation
P= πdts[(D/d)-C]
Where
P= drawing force, N
t= thickness of the blank material, mm
s= yield strength of the metal, MPa
C= constant to cover friction and bending, its value is 0.6 to 0.7.
For other shapes the above formula gives an approximation which can be used as a guide.
Blank Holding Force:
This force required depends on the wrinkling tendency of the cup which is very difficult to determine and hence it is obtained more by trial and error. The maximum limit is generally one-third of the drawing force.

## Slide 18
Ironing force:
In ironing the objective is to reduce the wall thickness of the cup, and hence no blank is required because the punch is fitted closely inside the cup. Neglecting the friction and shape of the die, the ironing force can be estimated by the following equation.
F= πd1t1savloge(t0/t1)
Where
F = ironing force, N
d1 = mean diameter of the shell after ironing
t1 = thickness of shell after ironing
t0= thickness of the shell before ironing
sav = average of tensile strength before and after ironing.
Air Vent:
An air vent is normally provided on the punch to reduce the possibility of formation of vaccum in the cups when it is stripped from the punch. The size of the air vent depends on the punch diameter

## Slide 19
Drawing Speed :
The speed with which the punch moves through the blank during drawing is termed as the drawing speed. This is very important parameter in drawing because the higher speeds are sometimes detrimental. Particularly harder and less ductile materials are likely to be excessively thinned out due to excessive drawing speeds.

## Slide 20
Punch Design:
The choice of the type of the punch and its design depends on the shape and size of the pierced or blanked contour and the work material. Large cutting perimeters require punches which are inherently rigid and can be mounted directly. Smalller size holes require punches which may have to be supported during the operation, and therefore need to have other mechanisms to join th punch holder. The punches can be broadly classified as: plain punches, pedestal punches, and punches mounted on punch plate.
Types of Punches:
Plain Punches:
Pedestal punches:
Punches Mounted in Punch Plates
Perforator type Punches:
Quill punches:

## Slide 21: WORKSHOP PRACTICE
Now we have a clear idea of the types of metals used. But this is not sufficient, we need to have the knowledge of the various kinds of tools for converting these materials into useful products.
Hand Tools
Common tools used for sheet metal working include:
• ·Standard Scale
• Trammels
• Circumference Rule
• Prick Punch
• Straight Edge
• Centre Punch
• Steels Square
• Hand Snip or Shear
• Scriber
• Stakes
• Semi-circular Protractor
• Hammers
• Dividers
• Hollowing Block

## Slide 22: Common types of joints used in sheet metalwork
Some of the common types of Sheet Metal Joints
(a) Lap joint, the most common type of general use
(b) Flush joint used where one face of the article is required to be level or flush.
(c) Edge over joint used for readily fixing bottoms
(d) Rivetted joint where in overlap is kept about six to eight times of the diameter of rivet
(e) Grooved joint wherein one edge of the sheet is folded down and the other up.
(f) Double grooved joint (inside type) is used to avoid projections on the outer surface of the job. It holds together firmly the edges of round or straight-sided jobs

## Slide 23: Types of joints used in sheet metal work are shown below

## Slide 24: SAFETY GUIDE FOR SHEET METAL WORKERS
There are certain things in your job that can lead to fatigue, discomfort, or pain when you do them repeatedly or without breaks. These include:
• Exerting force to perform a task or to use a tool.
• Working in positions such as bending, kneeling, stooping, twisting, and overhead reaching.
• Using awkward hand, wrist, elbow, or shoulder postures.
• Remaining in the same position for a long time with little or no movement.
• Continuous pressure from a hard surface or edge on any part of the body.
• Working in very hot or very cold temperatures produced by climate, equipment, or machines.
• Sitting on, standing on, or holding equipment or tools that vibrate.
In addition, stressful work situations can increase muscle tension and reduce awareness of proper work technique.
Most common injuries:
Back, Wrists and Hands, Knees, Neck and Shoulders

## Slide 27
THANK YOU